[image: image5.png]


                                         [image: image2]
	CHARACTER：

 1.Physical performance 
 a、Excellent mechanical properties
 b、Excellent thermal stability
 c、Low temperature soft good performance

 d、Good flame retardancy 
 e、Of high resistance to chemicals
 f、Chemistry stability is good
 b、Good resistance to high temperature of the engine fluid

 j、Excellent resistance to impact ability

 2.Electrical Properties 

 a、Electrical insulation good
 b、Good the dielectric properties

 3.Processing properties

 a、Using the hot extrusion processing
 b、Can be twisted pair and multi-core
 c、Good processing properties Harness

 d、Harness processing process good compatibility

 e、According to DIN standard design

 4.Environmental protection

 a、ROHS/REACH compliant
SHOULD BE USED：

 Apply to road vehicles with thin wall insulation single core no shielding low voltage cables
REFERENCE：

 DIN 72551-6,ISO6722

Outline：

.
	[image: image1]    Strands Tinned/Bare Copper
[image: image3]
[image: image4]

                        PVC Insulation 

road vehicles with thin wall insulation single core no shielding low voltage cables  FLRY-A
Wire structure description：

Conductor: Tinned /Bare copper ；
Insulation materials: PVC Insulation
Ground vehicles with low voltage electric system primary cable

Rated temperature: -40~105℃   rated voltage: 60Vac or 25Vdc
STYLE
mm2
Conductor size

(No./ mm)

±0.005mm
Conductor 

Dia.(mm)

Conductor resistance

20℃
（Ω/Km）
insulation

thickness

(mm)

Overall diameter

（mm）
Bare

tin.

Nom.
Nom. 
tolerance
FLRY-A
0.22
7/0.20
0.60
84.80
86.5
0.25

1.20

+0/-0.10

0.35
7/0.254
0.76
52.00
54.5
0.25
1.30
+0/-0.10

0.50
19/0.19
0.95
37.10
38.2
0.30
1.60
+0/-0.20

0.75
19/0.23
1.15
24.70
25.4
0.30
1.90
+0/-0.20

1.00
19/0.25
1.25
18.50
19.1
0.40
2.10
+0/-0.20

1.50
19/0.32
1.60
12.70
13.0
0.40
2.40
+0/-0.20

2.50
19/0.41
2.05
7.60
7.80
0.45
3.00
+0/-0.30

Marking：FLRY-A NO mm2 -40-105℃ 50V PVC QIFURUI
SAE COLOR SERIES
* STOCK COLOR CHART

00-BLACK
01-WHITE
02-RED
03-YELLOW
04-GREEN

05-BLUE
06-BROWN
07-GREY
08-ORANGE

09- VIOLET
PACKAGE

*PACKAGE

Part No.
Packing- Ft/roll
  

0.22~1.0mm2
□ 100M
□ 200M
□ 500M
■ 1000M
1.5~2.5mm2
□ 100M
□ 200M
■ 500M
□ 1000M
According to customer requirements for packaging packaging




�





�








Web site:www.qifurui.com                                                                                                         Tel:0755-33897988

Email:all@qifurui.com                                                                                                             Fax: 0755-33843991-3

This document belongs to the Shenzhen QFR Electronics Co., Ltd. all, the prohibition of unauthorized copying, transmission

